Facile synthesis of PVP coated silver nanoparticles and evaluation of its physico-chemical and antimicrobial and toxic activity

Francisco Nunes de Souza Netoa, Leonardo Antonio de Moraisa; Luiz Fernando Gorupb,c,d,e; Lucas da Silva Ribeirob; Tassia Joi Martinsb; Thayse Yumi Hosidaa; Patricia Francattob; Debora Barros Barbosaa; Emerson Rodrigues Camargob; Alberto Carlos Botazzo Delbema*

a State University of São Paulo (UNESP), Araçatuba Dental School, Department of Pediatric Dentistry and Public Health, Rua José Bonifácio 1193, Araçatuba – SP, 16015-050, Brazil.

b Federal University of São Carlos (UFSCar), Department of Chemistry, Interdisciplinary Laboratory of Electrochemistry and Ceramics (LIEC), Washington Luis Highway, Km 235, São Carlos – SP, 13565-905, Brazil.

c Federal University of Rio Grande -FURG, School of Chemistry and Food Science, Av. Italia km 8, Carreiros, Rio Grande, RS, 96203-900, Brazil.

d Federal University of Pelotas, Materials Engineering, Campus Porto, 96010-610, Pelotas, RS, Brazil.

e  Federal University of Alfenas, Institute of Chemistry, 37130-001, Alfenas-MG, Brazil.

Experimental

Synthesis of Silver Nanoparticles (AgNPs)

The solutions of silver nitrate (AgNO3) (AgNO3, 99.9% Sigma-Aldrich, Brazil 4.5 mmol) and PVP (PVP, Mw 10,000, (C6H9NO)n, 99% Sigma-Aldrich, Brazil, 4.5 mmol (molar number referent to PVP monomeric unit)) were prepared separately by dissolving the respective precursors in 50 mL of anhydrous ethanol (C2H5OH, Synth 99.8%, Brazil). Subsequently, the reaction system was kept under reflux and constant stirring for 4 h at 80 °C (Figure SI1). The experiments were carried out in order to obtain uniform particles with a narrow particle size distribution.

The experiments with different reactional conditions were carried out in a procedure similar to the one previously mentioned, and it was evaluated their effects on the size of AgNPs and their microbiological activity.

S1: Schematic representation of synthesis of silver nanoparticles in alcoholic medium.

Results

UV-Vis Spectroscopy (UV-Vis)

S2: UV–Vis spectra of synthesized AgNPs at different concentrations and average molecular weights of PVP. A: 10K; B: 40K; C 360K.

X-ray Diffraction (XRD)

S3: X-ray diffractograms of AgNPs at different concentrations and average molecular weights of PVP 10K.

Scanning Electron Microscopy (SEM)

S4: SEM micrographs of AgNPs and particle size distribution (2:1 Ag:PVP 10K).

S5: SEM micrographs of AgNPs and particle size distribution (4:1 Ag:PVP 10K).

Dynamic Light Scattering (DLS)

S6: Size distribution by number (%) of hydrodynamic diameter at different concentrations and average molecular weights of PVP 10K.

S7: Size distribution by number (%) of hydrodynamic diameter at different concentrations and average molecular weights of PVP 40K.

S8: Size distribution by number (%) of hydrodynamic diameter at different concentrations and average molecular weights of PVP 360K.